## Slide 1
What a dislocation runs into
from the lattice itself, to individual obstacles, to the structure that holds them
(a) Lattice friction and kink pairs
Peierls valleys
kink pair
dislocation line
the line sits in a valley and moves forward by throwing a kink pair into the next one
(b) Waiting at discrete obstacles
applied
stress
obstacles
bowed segment
break away,
or climb over
the segment stops, bows out, and waits until it gets past the obstacle
(c) The structure that stores dislocations
grain
sub-boundaries
(sub-grain, lath)
dislocations
coarse and fine particles
(d) Obstacle spacing sets the strength
spacing L
spacing L′
radius r
dislocation line
closer and larger obstacles mean a shorter free length and a harder material
Notes: Four-panel schematic: lattice friction and kink pairs, waiting at obstacles, the structure that stores dislocations, and obstacle spacing. Every element is a native, editable shape.

## Slide 2
A dislocation travels, then waits
every term in the model is a statement about how long a segment spends travelling and how long it spends held up
slip plane
glide direction
kink pair
held at a particle, the line bows out
forest junction
solutes collect while it waits
climbs over or breaks away,
and travels again
Travelling
Between obstacles the segment glides by nucleating kink pairs on screw dislocations and sweeping them sideways. This is slow and hard when it is cold, and almost free once the barrier is thermally overcome.
Waiting
At forest junctions, particles and boundaries the line stops and bows out. The longer it waits, the more solute atoms reach it and the stronger the pinning becomes.
Getting free
Two escapes compete at every obstacle: thermal activation past it, or climb over it. Whichever happens first releases the segment, and the travelling starts again.
Notes: The travel-and-wait picture behind the flow rule. All shapes are editable.

## Slide 3
The mechanisms in play
what sets the glide speed, what holds the line up, and what changes the structure while it deforms
Kink-pair glide
How fast the segment travels through the lattice between obstacles. Sets the low-temperature strength and its strong rate and temperature dependence.
Forest junctions
Other dislocations threading the slip plane. They act as a back stress the moving line has to push against everywhere.
Boundaries
Grain, sub-grain and lath boundaries. They store dislocations and shorten the distance a segment can travel before it is stopped.
Solute atmospheres
Interstitial solutes diffusing to a waiting segment. Slower deformation means more time to age, which is dynamic strain aging.
Particle detachment
Thermal activation lets a pinned segment break away from a second-phase particle once it has bowed out far enough.
Local climb
The other escape: the line climbs over the particle. It needs diffusion, so it takes over when it is hot and the loading is slow.
Recovery
Stored dislocations annihilate: by cross slip as the crystal deforms, and by climb, which keeps going whether or not it deforms.
Diffusional flow
Matter moving through the grains and along the boundaries rather than dislocations moving. A separate carrier that only matters at very low stress.
Notes: One card per mechanism. Colours match the schematics on the earlier slides.